PCR PET HY0801

Source Beverage bottle

Application Electronics, Spinning, Toys

Performance table

|  |  |  |
| --- | --- | --- |
|  | Testing standards |  |
| Melting point |  | ≥245 |
| Viscosity | ISO1628-5 | 00.67±0.03DL/g |
| Water content | ISO62 | ≤0.4% |
| Ash content | ISO3451 | ≤0.08% |
| L color value |  | ≥75 |
| B color value |  | ≤5 |
| Density | ISO1183 | 1.395±0.02g/cm³ |