PCR PBT

Source Optical cable, electrical appliance cover ，

Application Automotive, 3C products, communication, electrical appliances

Performance table

|  |  |  |
| --- | --- | --- |
|  | Testing standards |  |
| Melt Flow Index | ASTM D1238 |  35g/10min |
| Tensile strength | ASTM D638 | 50MPa |
| Elongation | ASTM D638 | 20% |
| Bending strength | ASTM D790 | 85MPa |
| Bending modulus | ASTM D790  | 2400MPa |
| Notched IZOD Impact | ASTM D256 | 150J/m |
| Density | ISO 1183 | 1.31g/cm3 |