PCR ABS

Source Toys、Automotive

Application Electronics, automotive, household appliances, tools, luggage

Performance table

|  |  |  |
| --- | --- | --- |
|  | Testing standards |  |
| Melt Flow Index | ASTM D1238 | 25g/10min |
| Tensile strength | ASTM D638 | 40MPa |
| Elongation | ASTM D638 | 15% |
| Bending strength | ASTM D790 | 65MPa |
| Bending modulus | ASTM D790 | 2200MPa |
| Notched IZOD Impact | ASTM D256 | 200J/m |
| Density | ASTM D792 | 1.05g/cm3 |