PCR-PP

Source Furniture, automotive, household appliances, tools

Application Packaging, pipeline

Performance table

|  |  |  |
| --- | --- | --- |
|  | Testing standards |  |
| Melt Flow Index |  ASTM D1238  |  4g/10min |
| Tensile strength | ASTM D638 | 25MPa |
| Elongation | ASTM D638 | 50% |
| Bending strength | ASTM D790 | 27MPa |
| Bending modulus | ASTM D790  | 800MPa |
| Notched IZOD Impact | ASTM D256 | 80J/m |
| Density | ASTM D792 | 0.9g/cm3 |