GF20PC

Source lampshade、Instrument panel cover、CD

Application Electronics, Automotive, Drones, Optical

Performance table

|  |  |  |
| --- | --- | --- |
|  | Testing standards | GF20 |
| Melt Flow Index | ISO 1133 | 15g/10min |
| Tensile strength | ISO 527 | 85MPa |
| Elongation | ISO 527 | 6% |
| Bending strength | ISO 178 | 110MPa |
| Bending modulus | ISO 178 | 3800MPa |
| Notched IZOD Impact | ISO 180 | 6KJ/m2 |
| Density | ISO 1183 | 1.33g/cm3 |
| GWIT |  | 960℃ |