PC/ABS AC3015

Source Instrument panel cover、Water bucket, lampshade ，

Application laptop

Performance table

|  |  |  |
| --- | --- | --- |
|  | Testing standards |  |
| Melt Flow Index | ASTM D1238 | 15 g/10min |
| Tensile strength | ASTM D638 | 60MPa |
| Elongation | ASTM D638 | 8% |
| Bending strength | ASTM D790 | 90MPa |
| Bending modulus | ASTM D790 | 3800MPa |
| Notched IZOD Impact | ASTM D256 | 120J/M |
| Density | ASTM D792 | 1.30g/cm3 |
| FR | UL94 | 1.5MM V0 |